| Head marking | Grade, material, and condition | Nominal size range (mm) | Proof strength (MPa) | Yield strength, min. (MPa) | Tensile strength, min. (MPa) | Core hardness (Rockwell) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Class 3.6 | 1.6–36 | 180 | 190 | 330 | B52–95 |
|  | Class 4.6 Low or medium carbon steel | 5–100 | 225 | 240 | 400 | B67–95 |
|  | Class 4.8 Low or medium carbon steel; fully or partially annealed | 1.6–16 | 310 | 340 | 420 | B71–95 |
|  | Class 5.8 Low or medium carbon steel; cold worked | 5–24 | 380 | 420 | 520 | B82–95 |
|  | Class 8.8 Medium carbon steel; quench and tempered | Under 16 (inc.) | 580 | 640 | 800 |  |
|  |  | 17–72 | 600 | 660 | 830 | C23–34 |
|  | Class 8.8 low carbon Low carbon boron steel; quench and tempered |  |  |  |  |  |
|  | Class 8.8.3 Atmospheric corrosion resistant steel; quench and tempered |  |  |  |  |  |
|  | ASTM A325M - Type 1 Medium carbon steel; quench and tempered | 12–36 |  |  |  |  |
|  | ASTM A325M - Type 3 Atmospheric corrosion resistant steel; quench and tempered |  |  |  |  |  |
|  | Class 9.8 Medium carbon steel; quench and tempered | 1.6–16 | 650 | 720 | 900 | C27–36 |
|  | Class 9.8 low carbon Low carbon boron steel; quench and tempered |  |  |  |  |  |
|  | Class 10.9 Alloy steel; quench and tempered | 5–100 | 830 | 940 | 1040 | C33–39 |
|  | Class 10.9 low carbon Low carbon boron steel; quench and tempered |  |  |  |  |  |
|  | Class 10.9.3 Atmospheric corrosion resistant steel; quench and tempered |  |  |  |  |  |
|  | ASTM A490M - Type 1 Alloy steel; quench and tempered | 12–36 |  |  |  |  |
|  | ASTM A490M - Type 3 Atmospheric corrosion resistant steel; quench and tempered |  |  |  |  |  |
|  | Class 12.9 Alloy steel; quench and tempered | 1.6–100 | 970 | 1100 | 1220 | C38–44 |
|  | A2 Stainless steel with 17–19% chromium and 8–13% nickel | Up to 20 |  | 210 minimum 450 typical | 500 minimum 700 typical |  |
|  | ISO 3506-1 A2-50 304 stainless steel-class 50 (annealed) |  |  | 210 | 500 |  |
|  | ISO 3506-1 A2-70 304 stainless steel-class 70 (cold worked) |  |  | 450 | 700 |  |
|  | ISO 3506-1 A2-80 304 stainless steel-class 80 |  |  | 600 | 800 |  |

For more information:  http://en.wikipedia.org/wiki/Screw