| Head marking | Grade, material, and condition | Nominal size range (in) | Proof strength (ksi) | Yield strength, min. (ksi) | Tensile strength, min. (ksi) | Core hardness (Rockwell) |
| --- | --- | --- | --- | --- | --- | --- |
|  | SAE Grade 0 | Strength and hardness is not specified |
|  | SAE grade 1 ASTM A30 Low carbon steel | 1⁄4–1-1⁄2 | 33 |  | 60 | B70–100 |
|  | ASTM A307 - Grade B Low or medium carbon steel | 1⁄4–4 |  |  | 60 minimum 100 maximum | B69–95 |
|  | SAE grade 2 Low or medium carbon steel | 1⁄4–3⁄4 | 55 | 57 | 74 | B80–100 |
|  |  | Greater than 3⁄4 | 33 | 36 | 60 | B70–100 |
|  | SAE grade 4 Medium carbon steel; cold worked | 1⁄4–1-1⁄2 |  | 100 | 115 |  |
|  | SAE grade 3[ Medium carbon steel; cold worked | 1⁄4–1 | 85 |  | 100 | B70–100 |
|  | SAE grade 5 Medium carbon steel; quench and tempered | 1⁄4–1 (inc.) | 85 | 92 | 120 | C25–34 |
|  |  | 1–1-1⁄2 | 74 | 81 | 105 | C19–30 |
|  | ASTM A449 - Type 1 Medium carbon steel; quench and tempered | 1–1-1⁄2 (inc.) | 74 |  | 105 | C19–30 |
|  |  | 1-1⁄2–3 | 55 |  | 90 | Brinell 183–235 |
|  | SAE grade 5.1 Low or medium carbon steel; quench and tempered | No. 6–1⁄2 | 85 |  | 120 | C25–40 |
|  | SAE grade 5.2 Low carbon martensitic steel; quench and tempered | 1⁄4–1 | 85 |  | 120 | C26–36 |
|  | ASTM A449 - Type 2 Low carbon martensitic steel; quench and tempered |  |  |  |  | C25–34 |
|  | ASTM A325 - Type 1 Medium carbon steel; quench and tempered | 1⁄2–1 (inc.) | 85 | 92 | 120 | C24–35 |
|  |  | 1–1-1⁄2 | 74 | 82 | 105 | C19–31 |
|  | ASTM A325 - Type 3 Atmospheric corrosion resistant steel; quench and tempered | 1⁄2–1 | 85 | 92 | 120 | C24–35 |
|  |  | 1–1-1⁄2 | 74 | 82 | 105 | C19–31 |
|  | ASTM A354 - Grade BC Medium carbon alloy steel; quench and tempered | 1⁄4–2-1⁄2 (inc.) | 105 | 109 | 125 | C26–36 |
|  |  | 2-1⁄2–4 | 95 | 99 | 115 | C22–33 |
|  | SAE grade 7 Medium carbon alloy steel; quench and tempered | 1⁄4–1-1⁄2 | 105 | 115 | 133 |  |
|  | SAE grade 8 Medium carbon alloy steel; quench and tempered | 1⁄4–1-1⁄2 | 120 | 130 | 150 | C32–38 |
|  | ASTM A354 - Grade BD Medium carbon alloy steel; quench and tempered | 1⁄4–2-1⁄2 (inc.) | 120 | 130 | 150 | C33–39 |
|  |  | 2-1⁄2–4 | 105 | 115 | 140 | C31–39 |
|  | SAE grade 8.2 Medium carbon boron martensitic steel; fully kilned, fine grain, quench and tempered | 1⁄4–1 | 120 |  | 150 | C33–39 |
|  | ASTM A490 - Type 1 Medium carbon alloy steel; quench and tempered | 1⁄2–1-1⁄2 | 120 | 130 | 150 minimum 170 maximum | C33–38 |
|  | ASTM A490 - Type 3 Atmospheric corrosion resistant steel; quench and tempered |  |  |  |  |  |
|  | 18-8 Stainless Stainless steel with 17–19% chromium and 8–13% nickel | 1⁄4–5⁄8 (inc.) |  | 40 minimum 80–90 typical | 100–125 typical |  |
|  |  | 5⁄8–1 (inc.) |  | 40 minimum 45–70 typical | 100 typical |  |
|  |  | Over 1 |  |  | 80–90 typical |  |

For more information:  http://en.wikipedia.org/wiki/Screw